# PROSOCO R-Guard® Joint & Seam Filler

# Specification for Fiber-Reinforced Fill Coat and Seam Treatment

Specifier Note:  The information provided below is intended to guide the Architect in developing specifications for products distributed and/or manufactured by PROSOCO, Inc. and should not be viewed as a complete source of information about the product(s). The Architect should always refer to the Product Data Sheet and Material Safety Data Sheet for additional recommendations and for safety information

Specifier Note:  Paragraph below is for PART 1 GENERAL, Quality Assurance.

# Mock-Ups

Apply to field-constructed mock-up assemblies illustrating material interfaces and seals. Use the manufacturer’s application instructions. Keep mock-ups available for inspection throughout the project.

Specifier Note:  Paragraphs below are for PART 2 PRODUCTS, Manufacturers and Products.

# Manufacturer

PROSOCO, Inc., 3741 Greenway Circle, Lawrence, KS 66046.  Phone: (800) 255-4255; Fax: (785) 830-9797.  E-mail:  CustomerCare@prosoco.com

# Product Description

PROSOCO R-Guard® Joint & Seam Filler fills openings and creates transitions where flexible reinforcement is required to bridge gaps and provide continuous support of fluid-applied flashing membranes, waterproofing or air barrier components. R-Guard Joint & Seam Filler is a single component, fiber-reinforced Silyl-Terminated-Polymer (STP) gun-grade detailing compound suitable for all climates.

Joint & Seam Filler bonds directly to damp or dry surfaces and eliminates the need for reinforcing tapes at sheathing joints, inside and outside corners. Appropriate for vertical or horizontal above-grade applications to concrete, masonry, natural stone, structural sheathing, architectural metals, painted metals, glass, PVC, FRP, EPDM and most other building materials.

# Typical Technical Data

FORM: pale red, viscous paste with mild odor

SPECIFIC GRAVITY: 1.4 to 1.5

pH: Not applicable

WEIGHT/GALLON: 11.8 pounds per gallon

TOTAL SOLIDS: 99 percent

FLASH POINT: No data

FREEZE POINT: No data

SHELF LIFE: 1 year in unopened, factory-sealed container

VOC: 30 grams per Liter, maximum. Complies with all known national, state and district AIM VOC regulations.

# Limitations

- Not for use as a liquid flashing membrane.

- Not for use in place of appropriate through-wall flashing.

- Not for use below grade or in locations which are continuously immersed in water.

Specifier Note:  Paragraphs below are for PART 3 EXECUTION, Installation.

# Installation

Before applying, read “Preparation” and “Safety Information” sections in the Manufacturer’s Product Data Sheet for R-Guard Joint & Seam Filler.  Refer to the Product Data Sheet for additional information about application.

Use R-Guard Joint & Seam Filler in concentrate. Do not dilute or alter. No mixing is required.

Application Instructions: Filling Joints, Seams and Cracks Detailing Fastener Heads and Around Penetrations

- Apply a bead of Joint & Seam Filler to all sheathing joints, seams and cracks then strike smooth with a DRY tool. Detail over wood knots, deep cracks or surface irregularities to complete the surface preparation.

- Use a DRY knife, trowel or spatula to spread the product 1 inch beyond the sheathing seams on each side to a thickness of 20 to 30 mils.

- Spot fastener heads and strike with a DRY tool.

- Allow to skin before installing other waterproofing or air barrier components.

SPECIFIER NOTE: Do not use soapy water when tooling or spreading.

SPECIFIER NOTE: Joint widths up to 3/8 inch may be treated without backer rod. Treat joints ranging from 3/8 to 1 inch with backer rod before applying Joint & Seam Filler. Joints larger than 1 inch must be structurally improved or addressed with R-Guard SureSpan EX transition extrusion.

Application Instructions: Detailing and Waterproofing Fastener Penetrations (Window and Door Penetrations)

- Apply a bead of Joint & Seam Filler in each corner of the rough opening and at the sheathing to stud transition, then strike smooth with a DRY tool.

- Use a DRY joint knife, trowel or spatula to tool and spread the product 1 inch beyond seam on each side to a thickness of 20 to 30 mils.

- Allow treated surfaces to skin over before installing R-Guard FastFlash®.

SPECIFIER NOTE: Do not use soapy water when tooling or spreading.

SPECIFIER NOTE: Joint widths up to 3/8 inch may be treated without backer rod. Treat joints ranging from 3/8 to 1 inch with backer rod before applying Joint & Seam Filler. Joints larger than 1 inch must be structurally improved or addressed with R-Guard SureSpan EX transition extrusion.

Application Instructions: Flashing Transitions

- Fasten R-Guard SS ThruWall or other flashing leg to the vertical wall surface using a bead of Joint & Seam Filler or conventional methods. Fill any voids between the flashing leg and the vertical wall with Joint & Seam Filler.

- Apply and tool Joint & Seam Filler as needed to direct water from the vertical wall to the face of the SS ThruWall or other flashing.

- Apply and tool Joint & Seam Filler at inside corners to ensure positive drainage.

- Allow treated surfaces to skin before installing R-Guard FastFlash®.

- Use Joint & Seam Filler to fill any remaining surface imperfections to provide positive drainage and continuous support of fluid-applied flashing membranes.

SPECIFIER NOTE: Do not use soapy water when tooling or spreading.

# Curing and Drying

At 70 degrees Fahrenheit (21 degrees Celsius) and 50 percent relative humidity, R-Guard Joint & Seam Filler skins within 30 minutes and dries in 4 hours. Surfaces treated with R-Guard Joint & Seam Filler are paintable with most paints after 2 hours.

SPECIFIER NOTE: R-Guard Joint & Seam Filler is moisture curing. Low temperatures and low relative humidity slow dry time. High temperatures and high humidity accelerate drying.

# Typical Coverage

Coverage varies based on surface texture and irregularities. Estimated coverage includes overlapping 1 inch on each side of the sheathing joint where the joint width varies from 0 to 0.25 inches.

- 60.5 to 93.5 linear feet per 29 ounce cartridge

- 38.5 to 60.5 linear feet per 20 ounce sausage

# Cleanup

Clean tools and equipment immediately with mineral spirits or similar solvent. Remove cured product mechanically with a sharp-edged tool.